| # PRODUCT DATA SHEET HDTMPA·K6 |  |  |
| --- | --- | --- |
| Synonyms | HDTMP hexapotassium salt |  |
| CAS Number | 38820-59-6;53473-28-2 |  |
| Einecs Number | 254-135-7;258-575-0 |  |
| Molecular Formula | C10H20K6N2O12P4 |  |
| Molecular weight | 718.7579 |  |
| Structural Formula |  |  |
| Product Grade | Industrial |  |
| Description & Application | HDTMPA K6 has a high solubility, which can prevent scaling salts from forming scales in water. It is a good calcium sulfate scale inhibitor, especially suitable for high alkali and high pH conditions. HDTMPA K6 is especially suitable for boiler water treatment and reverse osmosis membrane treatment.. |  |
| Safety Protection | Acidity, avoid contact with eye and skin, once contacted, flush with water. |  |
| Specification | Active content (as acid)% : 21.2-24.6 Active content (as salt)% : 31.0-36.0 Phosphorous acid(as PO33-) %：≤2.0 Phosphoric acid(as PO43-)%: ≥16 Chloride (as Cl-) %: ≤4 pH（1% solution）: 6.0-8.0 Fe(以Fe2+计),ppm:: ≤35 Density(20℃) g/cm3 : 1.21 – 1.31 Appearance：colorless to pale yellow transparent liquid |  |
| Package | 200L Drum, 1000L IBC or Bulk. Stored in cool and dry place. |  |
| Shelf Life | 1 year. |  |