| # PRODUCT DATA SHEET ATMP |  |
| --- | --- |
| Synonyms | Amino trimethylene Phosphonic acid |
| CAS Number | 6419-19-8 |
| Einecs Number | 229-146-5 |
| UN No. | 3261 |
| Molecular Formula | C3H12 NO9P3 |
| Molecular weight | 299.05 |
| Structural Formula |  |
| Product Grade | Industrial |
| Description & Application | A scale and corrosion inhibitor for cooling circulation water system and oilfield water pipeline in fields of thermal power plant and oil refinery plant; Metal chelate agent and color fixing agent for print and textile; Complexing agent for electron plate and water scale cleaning agent for metals. |
| Safety Protection | Acidity, avoid contact with eye and skin, once contacted, flush with water. |
| Specification | Active content (as acid)% : ≥95 Chloride (as Cl-)%: ≤1.0 Phosphorous acid %: ≤4.5 pH(1% solution): ≤ 2.0 Iron(as Fe) ppm: ≤35 Appearance：white crystal powder |
| Package | 25kg/bag.,Stored in cool and dry place. |
| Shelf Life | 1 year. |