**CHANGZHOU KOYE CHEMICAL CO.,LTD**

**Resist Salt**

Chemical Composition: Meta-Nitro Benzene sulfonic acid sodium salt

Formula Structure: 

Molecular formula:C6H4O5NSNa

Grade: Industrial products

Description: A yellow powder, soluble in water and acid, insoluble in some organic solvents, such as alcohol, cther, benzenc, etc.

|  |  |
| --- | --- |
| **Items** | **Specifications** |
| Diazo value (concentrated) | 90% min |
| PH value | 7-9 |
| Solubility | 25g/l non-turbid |
| Moisture | 3.0% max |
| Impurity | 0.2% max |

Usage:1. It is used as a resisting agent for dyeing and printing go avoid forming striation which appear on coloring fibers with dyestuffs in the process of dyeing textile fibers , and as an oxidizing agent for electroplating technique , andas an intermediate for dyestuffs to synthesize other kinds of dyestuffs , etc.

Packing: plastic bag containing 25kg net within the knit bag for export.

Storage: stored in dry place, prevent from water and fire.