|  |  |
| --- | --- |
| **PRODUCT DATA SHEET** **Acumur 3100** | |
| Synonyms | Acumur 3100 |
| Product Grade | Industrial |
| Description  & Application | Acumur 3100 is the most excellent scale dispersant in all cooling water treatment chemicals.It has good inhibition for dry-type iron oxide and hydrated iron oxide.It is also an excellent dispersant for all-organic cooling water system.Acumur 3100 can also be used as a phosphate or phosphonate corrosion inhibitor stabilizer.Acumur 3100 is applied to the cooling water and boiler water inhibitors; especially for pressurized conditions and contains iron, zinc and phosphate systems. |
| Safety Protection | Week acidity, avoid contact with eye and skin, once contacted, flush with water. |
| Specification | Solid content% : ≥43  Free Monomer%：≤0.5  pH（1% solution）: ≤3.0  Density(20℃) g/cm3 : ≥1.150  Appearance: Light yellow transparent liquid |
| Package | In 25Kg or 250Kg net plastic drums. Stored in cool and dry place. |
| Shelf Life | 10 Months. |