| # PRODUCT DATA SHEET Polyquaternium-39 |  |
| --- | --- |
| Synonyms | Dimethyldiallylammonium chloride acrylic acid acrylamide copolymer |
| CAS Number | 25136-75-8 |
| Einecs Number | 607-564-2 |
| UN No. |  |
| Molecular Formula | (C8H16N·C3H5NO·C3H4O2·C |
| Molecular weight |  |
| Structural Formula |  |
| Product Grade | Industrial |
| Description & Application | - To hair care products ·Contributes luster and a soft, silky feel ·Provides excellent slip, lubricity and snag-free wet combability without excessive buildup ·Imparts excellent dry combability ·Adds luster to dry hair ·Avoids the static ·Compatible with most anionic and amphoteric surfactants ·Provides superior conditioning properties for products with extreme PH ranges ·Suggested starting concentration: 2~10% - 2.To skin-care product ·Imparts a smooth, velvety feel; reduces tightness after drying skin ·Provides excellent moisturization ·Contributes lubricity which can help make skin care products easier to apply ·Liquid cleansing products acquire richer foam with improved stability ·Suggested starting concentration: 1~6% |
| Safety Protection |  |
| Specification | Appearance; colorless clear viscous liquid. Solid(%); 10±0.5%. P.H(1% water solution,25℃); 5–8. Viscosity; 5000–15000CPS/25℃. |
| Package | 125kg/200kg net in plastic drum |
| Shelf Life | 1year |